CEE*QUEST SGH50

CEE*QUEST SGH50 is a mixture of sodium glucoheptonate isomers and oligosaccharides.  The product is intended for use as a metals ion chelating agent under alkaline conditions.   The product will chelate calcium, magnesium, iron, copper, manganese and aluminum. This product is biodegradable.

PRODUCT DATA

| Calcium Chelation | 280 mg calcium carbonate per gram |
| --- | --- |
| Iron Chelation | 500 mg Fe3+ per gram |
| Odor | Sweet |
| Specific Gravity | 1.267 - 1.279 at 72oF |
| Density | 10.55 - 10.65 lbs/gal |
| Solids ( Minimum ) | 49.5% (ASTM-C494) |
| Ammonia | Less than 0.05% (500 ppm) |
| pH | 8 to 10.5 |
| Crystallization Point | Below 15oF |
| Solubility | Miscible with Water |
| Containers | Tank Cars, Tank Trucks, Drums |
| APPLICATIONS OR USES Alkaline metal cleaning, derusting and descaling. Bottle washing, paint stripping, aluminum finishing. Agricultural micronutrient formulations that do not contain orthophosphates where metal ion sequestration is needed. |

10/95