INDUSTRIAL GRADE

PHOSPHORIC ACID

62% H3PO4

|  | COMPONENT | TYPICAL ANALYSIS |
| --- | --- | --- |
| CHEMICAL | Phosphoric Acid (H3PO4) | 62% |
| SPECIFICATIONS | Solids | trace |
|  | Free Water | 32.7% |
|  | Aluminum ,Al2O3 | 0.50% |
|  | Iron, Fe2O3 | 0.64% |
|  | Magnesium, MgO | 0.19% |
|  | Sulfate, SO4 | 1.85% |
|  | Potassium, K | 0.13% |
|  | Fluoride, F | 0.13% |
|  | Calcium, CaO | 8 ppm |
| PHYSICAL |  |  |
| SPECIFICATIONS | Specific Gravity 75oF | 1.51 |
|  | Weight Per Gallon | 12.6 |

5/96